TWO-WAY SHAPE MEMORY EFFECT OF SPUTTERED Ni-rich Ni2MnGa FILMS

M. Ohtsuka, M. Matsumoto, K. Itakagi, A.A. Cherechukin1, E.P. Krasnoperov2

Institute of Multidisciplinary Research for Advanced Materials Processing, Tohoku University, Sendai 980-8577, Japan

1Institute of Radioengineering and Electronics of RAS, Moscow 101999, Russia

2Russian Research Centre Kurchatov Institute, Moscow, Russia

The Ni-rich Ni2MnGa films were deposited at 400 W using Ni52Mn24Ga24 target on an aluminium substrate with a radio-frequency magnetron sputtering apparatus. The thickness of the films is about 5 mm. The samples were annealed in vacuum at 1073 K for 36 ks and cooled in the furnace. The annealed films were fastened on a silica tube and then aged at 673 K for 3.6 ks in argon flow. The films show a two-way shape memory effect through structural phase transition and its reversion. The influence of a magnetic field on the temperature of the structural phase transition and on two-way shape memory effect is investigated. It is found that temperature hysteresis of the phase transition is about 7-9 K, the transition temperature increase caused by magnetic field is about 1 K/T. So it is possible to control structural phase transition and shape memory by magnetic field H=10 T switching off and on.

5. Phase Transitions and Critical Phenomena

Oral or poster presentation

Institute of Radioengineering and Electronics of RAS, Mokhovaya Str. 11, Moscow 101999, Russia

e-mail: cherechukin@mail.ru